The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep41S-5.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Solvent Resistant Adhesive Withstands Methylene Chloride, Alcohols and Fuels

Formulated for bonding, sealing, coating and encapsulation applications, Master Bond EP41S-5 is a room temperature curing epoxy that combines a high strength profile, superior electrical insulation values and exceptional chemical resistance. This system can be used in the aerospace, electronic, power, chemical processing, specialty OEM and other industries.

Well suited for coating pumps, tanks, storage vessels and piping, EP41S-5 is able to deliver long-term protection against a wide array of chemicals including acids, bases, alcohols, fuels and many solvents. Most noteworthy is its resistance to methylene chloride, a common stripping agent. This makes EP41S-5 ideal for tamper proofing applications in the electronic industry.

EP41S-5 offers convenient handling with a 100 to 25 mix ratio by weight. The mixed epoxy has good flow properties with a moderate viscosity of 25,000-30,000 cps. It bonds well to a wide variety of substrates including metals, composites, glass, ceramics, as well as many rubbers and plastics. EP41S-5 will cure at room temperature or more rapidly at elevated temperatures. Upon curing, this system is rigid, with a hardness of 85-95 Shore D. It has a tensile strength of 10,000-12,000 psi at room temperature. Additionally, EP41S-5 features reliable electrical insulation characteristics with a dielectric constant of 3.5 at 60 Hz and a volume resistivity greater than 1014 ohm-cm.

EP41S-5 is serviceable over the wide temperature range of -80°F to +300°F [-62°C to +149°C]. Its natural color is black, but can be formulated in additional colors. This solvent free system is available for use in ½ pint, pint, quart, gallon and 5 gallon container kits as well as double barrel cartridges that can be dispensed in gun applicators.

Master Bond Electrically Insulative Adhesives

Master Bond EP41S-5 is a moderate viscosity, high strength, two part epoxy with excellent chemical resistance. This room temperature curing system also has superior electrical insulation properties. Read more about Master Bond’s electrically insulative adhesives at http://www.masterbond.com/properties/electrically-insulative-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep41S-5

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #