The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/mastersil-151tc.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Highly Flexible Addition Cured Silicone Offers Low Thermal Resistance

Master Bond MasterSil 151TC was developed to improve thermal management for electronic assemblies in bonding and gap filling applications. This 100% solids silicone compound features a thermal conductivity of 10-12 BTU•in/ft²•hr•°F [1.44-1.73 W/(m•K)] and superior electrical insulation properties. Volume resistivity is >1014 ohm-cm. “This two component, room temperature curing formulation contains a special blend of ultra fine thermal conductive fillers and can be applied in very thin sections”, said Venkat Nandivada, manager of technical support. “This significantly enhances its heat transfer capabilities. Thermal resistance for MasterSil 151TC is an impressive 7-10 x 10-6 K•m2/W.”

Additionally this product was designed to guard against hostile environmental conditions. It has excellent resistance to water and can withstand exposure to rigorous vibration, impact, shock, thermal cycling, salt spray, and airborne contaminants. Shrinkage upon cure is low. MasterSil 151TC has good flow properties, an elongation of 90-110% and a Shore A hardness of 80-90. It adheres well to most substrates without the use of primers. Serviceability is from -65°F to +400°F.

MasterSil 151TC has a working life of 2-4 hours for a 100 gram batch at 75°F. Most importantly this composition has a low exotherm upon cure. The color of Part A is white, Part B is clear. This durable product can be dispensed on complex shapes and delivers cost effective, reliable long term performance. It may be used in LED lighting, automotive, semiconductor packaging, communication, consumer electronic and energy industries. MasterSil 151TC is available for purchase in ounce, ½ pint, pint, quart kits.

Master Bond Thermally Conductive Adhesives

Master Bond MasterSil 151TC is a highly flexible, temperature resistant two component silicone adhesive offering low thermal resistance and outstanding thermal conductivity. Read more about Master Bond’s thermally conductive adhesive systems at https://www.masterbond.com/properties/thermally-conductive-epoxy-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/mastersil-151tc

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #