The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/uv10tk40m

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

UV Curing Adhesive Passes NASA Low Outgassing Specifications

Master Bond UV10TK40M is a one part UV curable system, which is not oxygen inhibited, and can be used for bonding, sealing and coating applications. UV10TK40M is optically clear, with a refractive index of 1.55. It has a high glass transition temperature (Tg) of 135-140°C and is serviceable from -60°F to +450°F. Its hardness upon curing is 75-85 Shore D.

“Not only does it meet NASA low outgassing specifications, but this system also withstands 1,000 hours at 85°C/85% RH. Its Shore D hardness was not adversely affected even after exposure to elevated temperatures and high relative humidity”, says Rohit Ramnath, Senior Product Engineer. UV10TK40M cures in 20-30 seconds when exposed to a UV light source emitting at a wavelength of 320-365 nm with 20-40 milliwatts per cm².

UV10TK40M bonds well to glass, surface treated metals and plastics such as polycarbonates and acrylics.  UV10TK40M is recommended in fiber-optic, optical, opto-electronic and electronic applications where heat resistance and a moderate viscosity are needed. The product is available in 1/2 pints, pints, quarts, gallons and syringes.

Master Bond UV Curable Adhesives

Master Bond UV10TK40M is a UV curing adhesive with a high Tg that is NASA low outgassing approved. Read more about Master Bond’s UV curable adhesives at https://www.masterbond.com/products/uv-curable-systems or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/newsrelease/uv10tk40m

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #